For making EL panel

- Raw material

- EL pigment

- Silver paste

- Special Barium titanate pigment for EL pigment

- Special glue(A/B glue) for EL pigment

- Glass film for electric conduction

- Thin coating film

- Process

- dry the EL pigment under 80 degrees in the oven

- making paste with EL pigment: mix EL pigment with glue, control the viscosity and get rid of debubbles

- print the glass film(for electric conduction) with mixed paste

- dry the glass film with printed layer in the oven

- making paste with Barium titanate pigment, control the viscosity and get rid of debubbles.

- Print the glass film(printed with EL pigment paste) with paste mixed with Barium titanate pigment.

- Dry the panel with printed layers in the oven

- Print the panel with silver paste

- Dry the panel in the oven

- Weld the electrodes on the panel

- Coat the panel with plastic protection film